# Support Information

Fig. S1 HRTEM image of CQDs

Fig. S2 HRTEM image of COM

Fig. S3 SEAD of COM, NOM, and TMO.

It can be seen that the basic diffraction ring shapes of NOM and TMO are consistent, and there is no significant change in the crystal planes. Therefore, it further explains that the improvement in COM's performance is due to the introduction of CQDs rather than changes in its morphology and structure.

Fig.S4 The average Young's modulus of TMO, NOM, and COM.

Fig. S5 (a) Raman spectra (1200-2000 cm-1), and (b) the FTIR of TMO, NOM, and COM

Table. S1 Comparison with Other Modified AZIBs Cathode Materials

| Materials | Conductivity (S cm-1) | Rate Capability | Reference |
| --- | --- | --- | --- |
| COM | 7.63×10-5 | 298.5 mA h g-1 at 1.0 A g-1 | This work |
| Pristine MnO2 | ~10-6 to 10-5 | Low | [1] |
| MnO-CNT@C3N4 | - | 209 mA h g-1 at 0.8 A g-1 | [2] |
| NVO0.3-350 | - | 465.9 mA h g-1 at 0.5 A g-1 | [3] |
| cCNTs-Bi/MnO2 | Higher than 2.21×10-⁵ | 104.5 mA h g-1 at 1.0 A g-1 | [4] |
| CNTs-MnO2 | - | 167 mA h g-1 at 1.0 A g-1 | [5] |
| NVOH_10 %CNT | 11.96 | 425.7 mA h g-1 at 0.5 A g-1 | [6] |
| ZMO/CNTs | 3.5×10-2 | 220.3 mA h g-1 at 0.1 A g-1 | [7] |
| CNTs@MnO2-25% | - | 183.5 F g⁻¹ at 0.1 F g-1 | [8] |
| MnO2@CeO2 | - | 355 mA h g-1 at 1 A g-1 | [9] |
| Zn-MnO2@NC | - | 325 mA h g-1 at 0.1 A g-1 | [10] |

References

[1]	H. Zhang, Z. Huang, Y. Du, D. Zha, L. Zhou, Y. Gong, J. Wang, L. Wang, Z. Gong, H. Zhang, Q. Zhang, Z. Liu, Manganese dioxide as cathode for aqueous zinc-ion batteries: reaction mechanisms, optimization strategies and further prospects, Microstructures 5 (2025) 2025091. https://doi.org/10.20517/microstructures.2024.193.

[2]	X. Xiao, T. Wang, Y. Zhao, W. Gao, S. Wang, A design of MnO-CNT@C3N4 cathodes for high-performance aqueous zinc-ion batteries, Journal of Colloid and Interface Science 642 (2023) 340–350. https://doi.org/10.1016/j.jcis.2023.03.164.

[3]	J. Feng, S. Wang, H. Yuan, Y. Zhang, S. Wang, Defect-engineered ammonium vanadate nanosheets with expanded interlayers for high-rate aqueous zinc ion batteries, Chemical Engineering  Journal 520 (2025) 166000. https://doi.org/10.1016/j.cej.2025.166000.

[4]	D. Zhu, H. He, C. Lu, C. Huang, G. Chang, Y. Qian, Q. Tang, A. Hu, X. Chen, J. Liu, Bismuth-loaded carbon nanotubes supporter inducing persistent Mn2+ deposition for enhanced stability of MnO2 cathodes in aqueous zinc-ion batteries, ChemSusChem (2025) e202402768. https://doi.org/10.1002/cssc.202402768.

[5]	Y. Fan, M. Xu, Q. Li, M. Liu, X. Zhang, P. Chu, B. Zhang, H. Zhou, Y. Zhao, C. Liu, Carboxyl-CNTs act as “defensive shield” to boost protonInsertion for stable and fast-charging aqueous Zn-Mn batteries, Small (2025) 2501454. https://doi.org/10.1002/smll.202501454.

[6]	M. Liu, X. Ren, Z. Gan, M. Sun, Z. Li, Constructing a high-loading cathode via the synergistic effect of carbon nanotubes and ammonium vanadate for high-rate and long-cycle aqueous  zinc-ion batteries, Journal of Alloys and Compounds 1042 (2025) 184149. https://doi.org/10.1016/j.jallcom.2025.184149.

[7]	F. Gao, B. Mei, X. Xu, J. Ren, D. Zhao, Z. Zhang, Z. Wang, Y. Wu, Y. Zhang, Rational design of ZnMn2O4 nanoparticles on carbon nanotubes for  high-rate and durable aqueous zinc-ion batteries, Chemical Engineering Journal 448 (2022) 137742. https://doi.org/10.1016/j.cej.2022.137742.

[8]	Z. Xu, Z. Pang, S. Alshammari, X. Yan, H.K. Thabet, X. Jiang, Z.M. El-Bahy, X. Xu, L. Yu, Ultrathin MnO2 nanosheets/carbon nanotubes heterostructures via electrostatic self-assembly for high-efficiency capacitive deionization, Chemical Engineering Journal 522 (2025) 166426. https://doi.org/10.1016/j.cej.2025.166426.

[9] M. Xie, R. Wang, N. Wang, Q. Zhang, X. Zhang, C. Feng, L. Huang, Y. Xu, Y. Jiao, J. Chen, MnO2@CeO2 Composite Cathode for Aqueous Zinc-ion Batteries: Enhanced Electrical Conductivity and Stability through Mn-O-Ce Bonds, Journal of Materials Chemistry A 11 (2023) 21927-21936. https://doi.org/10.1039/D3TA04837C.

[10] X. Li, Q. Zhou, Z. Yang, X. Zhou, D. Qiu, H. Qiu, X. Huang, Y. Yu, Unraveling the role of nitrogen-doped carbon nanowires incorporated with MnO2 nanosheets as high performance cathode for zinc ion batteries, Energy & Environmental Materials 6 (2022) e12378. https://doi.org/10.1002/eem2.12378.

Fig.S6 (a-c) The CQDs solution remaining on the teflon-lined lid fluoresces blue when irradiated by an ultraviolet lamp. (d) Write on toilet paper with CQDS solution (e) Toilet paper can still glow blue after being soaked in water.

1.0 g of citrate monohydrate and 0.5 g of urea were mixed in 25 mL of ultrapure water, and then the mixture was transferred to a polytetrafluoroethylene-lined medium for hydrothermal heating for 6 h. After cooling to room temperature, the mixture was filtered through a 0.22 μm microporous filter membrane, and the brown solution obtained was the CQDs solution. The solution fluoresces blue under ultraviolet light, as shown in Fig. S4a-c. To prove the stability of the CQDs solution, we dipped a small amount of CQDs into the toilet paper and wrote on it. Even after the CQDs solution was soaked in water, it could still emit blue fluorescence under ultraviolet irradiation, as shown in Fig. S4d-e.