Dual-ion (K⁺/Cu²⁺) Intercalated δ-MnO₂ as an Advanced Cathode Material for High Performance Aqueous Zinc-Ion Batteries

Chao Duana,b, Guizhao Zhu a,b, Yiyin Zhanga,b, Yawei Lia,b, Haixiang Huanga,b, Bogu Liua,b, Tingting Xua,b, Xiaohong Chena,b, Hong Zenga,b, Ying Wua,b*

a School of Energy Power and Mechanical Engineering, North China Electric Power University. No.2 Beinonglu Changping District, Beijing 102206, China

b Institute of Energy Power Innovation, North China Electric Power University, No. 2 Beinonglu Changping District, Beijing 102206, China

*Corresponding author.

Email: yingwu2000@hotmail.com, wuying@ncepu.edu.cn

Fig. S1 SEM image of K-MO.

Fig. S2 TEM image of KCu-MO.

Fig. S3 HRTEM image of K-MO.

Fig. S4 Cycling performance of KCu-MO, KCu-MO-0.5, KCu-MO-2 and K-MO electrodes at 0.1 A g-1 current density.

Fig. S5 Cycling performance of KCu-MO, KCu-MO-0.5, KCu-MO-2 and K-MO electrodes at 0.5 A g-1 current density.

Fig. S6 GCD curves at various current densities of K-MO.

Fig. S7 Comparison diagram of power density and energy density of KCu-MO compared to other reported cathode materials.

Fig. S8 GITT curve and diffusion coefficient of K-MO .

Fig. S9 GCD curve of KCu-MO at 0.1 A g-1 and related different charge-discharge states.

Fig. S10 Ex-situ XPS spectra of O 1s.

| Material | K-MO | KCu-MO |
| --- | --- | --- |
| Mn4+ peak area ratio fitted (%) | 28.04% | 21.56% |

Table S1 Fitted Mn4+ XPS peak area ratio of the samples.

| Sample | K(wt %) | Cu(wt %) | Mn(wt %) |
| --- | --- | --- | --- |
| KCu-MO | 6.6667% | 5.3339% | 48.4327% |

Table S2 ICP-OES element contents analysis of KCu-MO

| Materials | Electrolyte | Specific capacity | Cycling performance | Ref. |
| --- | --- | --- | --- | --- |
| MnO2@AEPA | 2M ZnSO4+ 0.1M MnSO4 | 223 mA h g-1 at 0.5 A g-1 | 97% after 1700 cycles at 1A g-1 | [1] |
| α-Mn2O3 | 2M ZnSO4+ 0.2M MnSO4 | 225 mA h g-1 at 0.05A g-1 | 53.3% after 1700 cycles at 2A g-1 | [2] |
| β‐MnO2-TA | 3M Zn(CF3SO3)2 + 0.1M Mn(CF3SO3)2 | 268.24 mA h g-1 at 0.1 A g-1 | 86.77% after 50 cycles at 0.1 A g-1 | [3] |
| Mo-MnO2 | 2M ZnSO4+ 0.2M MnSO4 | 222.8 mA h g-1 at 0.1 A g-1 | 82.6% after 1000 cycles at 2A g-1 | [4] |
| NS-MnO2 | 2M ZnSO4+ 0.1M MnSO4 | 295 mA h g-1 at 0.2 A g-1 | 94% capacity after 1500 cycles at 1A g-1 | [5] |
| K-δ-MnO2 | 2M ZnSO4+ 0.1M MnSO4 | 282.8 mA h g-1 at 0.3 A g-1 | over 50% after 1000 cycles at 2A g-1 | [6] |
| Se, P co-doping MnO2 | 2M ZnSO4+ 0.2M MnSO4 | 295 mA h g-1 at 0.5 A g-1 | 66% after 1000 cycles at 1 A g-1 | [7] |
| This work | 2M ZnSO4+ 0.1M MnSO4 | 257.49 mA h g-1 at 0.5 A g-1 | 84% after 5000 cycles at 1 A g-1 |  |

Table S3 Performance comparison of AZIBs with manganese oxide-based materials as cathodes.

|  | Rs/Ω | Rct/Ω |
| --- | --- | --- |
| KCu-MO | 2.043 | 262.4 |
| K-MO | 2.213 | 469.9 |

Table S4 Impedance value based on equivalent ciruit diagram fitting

Reference

[1] X. He, M. Kwon, J. Chung, K. Lee, Y. Choi, Y. Im, J. Jang, Y. Choi, H.J. Yoon, Self-assembled molecular layers as interfacial engineering nanomaterials in rechargeable battery applications,Small 20 (2024) 2403537.

[2] M. Mao, X.X. Wu, Y. Hu, Q.H. Yuan, Y.B. He, F.Y. Kang, Charge storage mechanism of MOF-derived Mn2O3 as high performance cathode of aqueous zinc-ion batteries, Journal of Energy Chemistry 52 (2021) 277-283.

[3] S. Paik, I. Choi, S. Lee, K.W. Nam, Chelating effects of polyphenolic biomolecules to improve β-MnO2 cathode performance for aqueous rechargeable zinc-ion batteries, Acs Applied Materials & Interfaces 16 (2024) 50775-50784.

[4] Z.H. Zheng, G.C. Yang, J. Yao, J.Y. Li, J.J. Zheng, Z. Wu, Y. Gan, C. Wang, L. Lv, H.Z. Wan, C. Chen, H.B. Wang, L. Tao, J. Zhang, H. Wang, High-valence molybdenum promoted proton migration and inhibited dissolution for long-life aqueous Zn-MnO2 batteries, Applied Surface Science 592 (2022) 153335.

[5] J. Liang, Y. Zhao, L. Ren, M. Li, Q. Zhang, Y. Wang, X. Sun, M. Chuai, X. Wang, W. Liu, Dual anions doping enhanced conductivity and stability of layered δ-MnO2 cathode for aqueous zinc-ion battery, Advanced Functional Materials 35 (2025) 2501135.

[6] Q.X. Xie, G. Cheng, T. Xue, L.H. Huang, S.H. Chen, Y. Sun, M. Sun, H.Z. Wang, L. Yu, Alkali ions pre-intercalation of δ-MnO2 nanosheets for high-capacity and stable Zn-ion battery, Materials Today Energy 24 (2022) 100934.

[7] K. Ma, S. Ge, R. Fu, C. Feng, H. Zhao, X. Shen, G. Liang, Y. Zhao, Q. Jiao, Uncovering Se, P co-doping effect in MnO2 toward high-performance aqueous zinc-ion batteries, Chemical Engineering Journal 484 (2024) 149525.