Supplementary Materials for

Ti4+-induced dual-functional α-MnO2 nanowires: boosting transport kinetics and interfacial optimization for aqueous zinc-ion batteries

Min Wanga, Tianyi Lia, Yuncheng Huanga, Xin Liua, Yixuan Lianga,Wen Zhanga, Guoqing Yanga, Fan Suc, Wei Zhanga, Chuan Dinga, Qilin Gud, Chao Huangfua,*, Hailin Shena,*, Zhenghui Panb,*

a School of Chemical Engineering and Materials, Changzhou Institute of Technology, Changzhou 213032, P. R. China

b School of Materials Science and Engineering, Tongji University, Shanghai 201804, P. R. China

c Advanced Analysis and Testing Center, Nanjing Forestry University, Nanjing 210037, P. R. China

d State Key Laboratories of Materials-Oriented Chemical Engineering, NJTECH University Suzhou Future Membrane Technology Innovation Center, College of Chemical Engineering, Nanjing Tech University, Nanjing, 211816, P. R. China

*Corresponding author: huangfc@czu.cn; shenhailin@czu.cn;

zhenghuipan@tongji.edu.cn

Figure S1 The refined XRD pattern of pristine α-MnO2 material.

Table S1 Calculated parameters of the pristine and Ti-doped α-MnO2 material.

|  | a/Å | b/Å | c/Å | V/(Å3) | Rp | Rwp |
| --- | --- | --- | --- | --- | --- | --- |
| pristine | 9.8652 | 9.8652 | 2.8617 | 278.51 | 5.64% | 7.08% |
| Ti-doped | 9.8615 | 9.8615 | 2.8625 | 278.38 | 6.12% | 7.17% |

Figure S2 XPS wide spectra of as-prepared Ti-doped and pristine α-MnO2 material.

Figure S3 FESEM images of pristine and Ti-doped α-MnO2 materials.

Figure S4 The electrochemical properties of as-prepared pristine α-MnO2 electrodes in 1M ZnSO4 + 0.1Mn MnSO4 aqueous electrolyte. (a) CV curves at 0.2 mV·s-1; (b) CV curves at various scan rates; (c) the relationship of peak current(i) and scan rate (ν) in the Figure S4b; (d) Galvanostatic charge/discharge profiles in initial three cycles at 100 mA·g-1 between 1.0 and 1.8 V.

Figure S5 Galvanostatic charge/discharge profiles at the 200th cycle at 100 mA·g-1 between 1.0 and 1.8 V.

Figure S6 FESEM images of the Ti-doped (a-b) and pristine (c-d) α-MnO2 electrodes before cycling.