Supporting Information

Dual-cations modulating δ-MnO2 as a high-performance cathode material for aqueous zinc-ion batteries

Haixiang Luoa, Hui-Juan Zhanga,*, Yiming Taoa, Zhu Hea, Zhengyu Lia, Yuhua Xuea

a School of Materials and Chemistry, University of Shanghai for Science and Technology, 516 Jungong Rd, Yangpu 200093, Shanghai, China

*E-mail address: hjzhang@usst.edu.cn.

1. Material characterizations

To analyze the crystal structure, X-ray diffraction (XRD) was conducted on a Bruker X-ray diffractometer (D8 Advance) at a range of 10°-80° with a scan rate of 5° per minute. Scanning electron microscopy (SEM) images were analyzed on ZEISS GeminiSEM 300. Transmission electron microscopy (TEM), high resolution transmission electron microscope (HR-TEM), high angle angular dark field-scanning transmission electron microscopy (HAADF-STEM) and its elemental mapping images were conducted on board FEI Talos F200X. X-ray photoelectron spectroscopy (XPS) measurements were performed on a Thermo Scientific K-Alpha.

2. Electrochemical measurements

Electrochemical performance was evaluated by assembling CR2032 coin cells. The cathode materials, acetylene black (ACET), and polyvinylidene fluoride (PVDF) were mixed in a ratio of 8:1:1 and dissolved in N-methyl-2-pyrrolidone (NMP) to prepare a slurry. The slurry was then coated onto stainless steel foil and dried under vacuum at 80°C for 8 hours. Zinc foil, glass fiber membrane (GF/A, Whatman), and a 2.0 M ZnSO4 aqueous solution with 0.2 M MnSO4 were used as the anode, separator, and electrolyte, respectively. Galvanostatic charge-discharge (GCD) tests were conducted at various current densities within a voltage range of 0.8-1.8 V using a NEWARE battery testing system. Cyclic voltammetry (CV) and electrochemical impedance spectroscopy (EIS) were measured using a CHI 660E electrochemical workstation. The CV curves were recorded at different scan rates between 0.8 and 1.8 V. The frequency range for EIS testing was 0.01-106 Hz with an amplitude of 5 mV.

Fig. S1 Rate preformances of FCMO with different Fe dopings.

Fig. S2 Rate preformances of FCMO with different Co dopings.

Table S1. Comparison of electrochemical properties of FCMO with other reported Mn-based cathode materials.

| Cathode | Capacity/(mAh·g-1) | Retention/cycles/rate | References |
| --- | --- | --- | --- |
| FCMO | 371.1 (0.1 A g-1) | 94.7%/1000/1 A g-1 | This work |
| Cr-MnO2 | 229.2 (0.1 A g-1) | 86%/300/0.1 A g-1 | [1] |
| α-MnO2@ZIF-67 | 313.4 (0.1 A g-1) | 65%/1500/1 A g-1 | [2] |
| W-MnO2 | 240.6 (0.1 A g-1) | 79.8%/1000/1 A g-1 | [3] |
| ε-MnO2/CPAN | 288.6 (0.2 A g-1) | 90%/1000/1 A g-1 | [4] |
| MnO2@CODs | 160 (0.1 A g-1) | 95.4%/500/1 A g-1 | [5] |
| Alx-MnO2 | 327.9 (0.2 A g-1) | 87%/1000/1 A g-1 | [6] |
| CNx/MnO2 | 249 (0.1 A g-1) | 77%/500/1 A g-1 | [7] |
| MgMn2O4 | 269 (0.1 A g-1) | 80%/500/0.5 A g-1 | [8] |
| F-MO | 288 (0.1 A g-1) | 96%/200/0.5 A g-1 | [9] |
| Ag0.4Mn8O16 | 227 (0.1 A g-1) | 50%/800/1 A g-1 | [10] |
| NS-MnO2 | 295 (0.2 A g-1) | / | [11] |
| NCMO | 313.4 (0.1 A g-1) | 97.4%/700/1 A g-1 | [12] |
| Se, P-MnO2 | 366.6 (0.1 A g-1) | / | [13] |
| Mo, P-MnO2 | 367.6 (0.1 A g-1) | / | [14] |
| Na0.08MnO2·0.57H2O | 368 (0.1 A g-1) | 83.7%/500/0.5 A g-1 | [15] |
| WKMO | 315(0.2 A g-1) | / | [16] |

Fig. S3 CV curves of δ-MnO2 at various current densities.

Fig. S4 Logarithmic plots of peak current (log i) versus scan rate (log v).

Fig. S5 Various contribution ratios of capacitance at different scanning rates in δ-MnO2.

Table S2. The fitting results of Nyquist plots for δ-MnO2 and FCMO.

|  | δ-MnO2 | FCMO |
| --- | --- | --- |
| R1/ohm | 6.958 | 3.422 |
| R2/ohm | 38.86 | 24.09 |
| R3/ohm | 201.7 | 85.87 |

References

[1] X. Ding, Y. Wen, C. Qing, Y. Wei, P. Wang, J. Liu, Z. Peng, Y. Song, H. Chen, Q. Rong, Cr-induced enhancement of structural stability in δ-MnO2 for aqueous Zn-ion batteries, Journal of Alloys and Compounds 986 (2024) 174041-174049.

[2] M. Bai, S. Li, C. Zhang, Y. Liu, Z. Wen, J. Sun, Novel composite cathode material α-MnO2@ZIF-67 for high performance aqueous rechargeable Zn-ion battery, Journal of Electroanalytical Chemistry 957 (2024) 118104-118113.

[3] Y. Gan, P. Shi, J. Pan, Y. Yang, J. Yao, L. Lv, H. Wan, H. Wang, High valence tungsten driven high stability phase and conductivity γ-MnO2 cathodes for durable aqueous zinc ion batteries, Journal of Energy Storage 127 (2025) 117176-117184.

[4] W. Fu, Y. Hou, L. Zhang, T. Ma, G. Duan, S. Yang, 3D ε-MnO2/electrospun carbon fiber cathodes for aqueous zinc-ion batteries, New Journal of Chemistry 49 (2025) 11254-11260.

[5] F. Zhang, H. Pan, L. Shuai, Y. Zheng, X. Huang, T. Wang, J. Yu, D. Wu, J. Dou, X. Chen, Coal-derived carbon quantum dots modified MnO2 nanowires as cathode for enhanced aqueous zinc-ion battery, Diamond and Related Materials 157 (2025) 112565-112574.

[6] Y. Zhao, S. Zhang, Y. Zhang, J. Liang, L. Ren, H.J. Fan, W. Liu, X. Sun, Vacancy-rich Al-doped MnO2 cathodes break the trade-off between kinetics and stability for high-performance aqueous Zn-ion batteries, Energy & Environmental Science 17 (2024) 1279-1290.

[7] Z. Ni, L. Zhao, H. Zhao, C. Jin, B. Ge, W. Li, In-situ growth of MnO2 nanorods on CN generates a heterostructure with the stability for zinc ion battery, Journal of Alloys and Compounds 967 (2023) 171834-171841.

[8] V. Soundharrajan, B. Sambandam, S. Kim, V. Mathew, J. Jo, S. Kim, J. Lee, S. Islam, K. Kim, Y.-K. Sun, J. Kim, Aqueous Magnesium Zinc Hybrid Battery: An Advanced High-Voltage and High-Energy MgMn2O4 Cathode, ACS Energy Letters 3 (2018) 1998-2004.

[9] D. Wang, Z. Liu, X.-W. Gao, Q. Gu, L. Zhao, W.-B. Luo, Massive anionic fluorine substitution two-dimensional δ-MnO2 nanosheets for high-performance aqueous zinc-ion battery, Journal of Energy Storage 72 (2023) 108740-108746.

[10] F.W. Fenta, B.W. Olbasa, M.-C. Tsai, N.T. Temesgen, W.-H. Huang, T.M. Tekaligne, Y. Nikodimos, S.-h. Wu, W.-N. Su, H. Dai, B.J. Hwang, Structural engineering of α-MnO2 cathode by Ag+ incorporation for high capacity aqueous zinc-ion batteries, Journal of Power Sources 548 (2022) 232010-232018.

[11] J. Liang, Y. Zhao, L. Ren, M. Li, Q. Zhang, Y. Wang, X. Sun, M. Chuai, X. Wang, W. Liu, Dual Anions Doping Enhanced Conductivity and Stability of Layered δ‐MnO2 Cathode for Aqueous Zinc-Ion Battery, Advanced Functional Materials 35 (2025) 1-10.

[12] J. Zeng, Z. Zhang, Y. Chen, G. Peng, M. Zhao, Y. Zhou, K. Bai, H. He, Boosting the synergistic activaion of δ-MnO2 as cathode for aqueous zinc-ion batteries through Ni, Co co-doping, Journal of Electroanalytical Chemistry 973 (2024) 118682-118692.

[13] K. Ma, S. Ge, R. Fu, C. Feng, H. Zhao, X. Shen, G. Liang, Y. Zhao, Q. Jiao, Uncovering Se, P co-doping effect in MnO2 toward high-performance aqueous zinc-ion batteries, Chemical Engineering Journal 484 (2024) 149525-149534.

[14] K. Ma, G. Liang, Q. Jiao, H. Jin, Y. Su, N. Li, J. Li, Z. Xiong, C. Feng, Y. Zhao, Unlocking Mo, P co-doping to boost proton intercalation in MnO2 as a high-performance cathode material for aqueous zinc-ion batteries, Journal of Materials Chemistry C 13 (2025) 4727-4736.

[15] G. Liu, Z. Ye, Z. Jiang, P. Zhou, Z. Li, Q. Luo, W. Li, Z. Huang, L. Liu, Sodium-Ion/Crystal Water Cointercalated δ-MnO2 with Improved Performance for Aqueous Zinc-Ion Batteries, ACS Applied Energy Materials 7 (2024) 9746-9755.

[16] G. Miao, Z. Wang, F. Sun, Y. Liu, F. Lin, Y. Fang, X. Yang, P. Li, X. Qu, Modulating the interlayer H+ migration in MnO2 via W and K co-doping engineering to high-capacity aqueous zinc-ion batteries, Journal of Colloid and Interface Science 693 (2025) 137636-137644.